# MRPL ASSET INTEGRITY & INSPECTION DIVISION

FINAL INTERNAL INSPECTION REPORT — API 510 (FIIR-SE-01)

# 1. Equipment & Metallurgy Particulars

Vessel Tag: V-102 (Vacuum Column Overhead Accumulator) | Material: SA-516 Gr. 70 + 316L Clad

Design Temp / Press: 220°C @ 4.5 bar-g | Joint Efficiency E = 1.0 (Full Radiography)

# 2. Ultrasonic Thickness & Corrosion Rate Evaluation

• Nominal Thickness: 12.0 mm | Minimum Required (t_min): 8.4 mm

• Actual Measured Thickness (t_act): 10.2 mm | Long-Term Corrosion Rate: 0.12 mm/year

• Remaining Life: (10.2 - 8.4) / 0.12 = 15.0 Years | Next Inspection Due: 7.5 Years (API 510 Half-Life)