# MANGALORE REFINERY AND PETROCHEMICALS LIMITED

EXECUTIVE APPROVAL NOTE / MOP&NG STATUTORY SUBMISSION

───────────────────────────────────────────────────────

| Unit / Location: | Crude Distillation Unit (CDU-1) - Furnace F-101 |
| --- | --- |
| Inspection Date: | 2026-08-30 |
| Refinery SOP Reference: | SOP-MRPL-FURNACE-01 (Clause 4.1.2) |
| Classification: | URGENT / MANDATORY OPERATIONAL ACTION |

# 1. Executive Anomaly Summary

During routine ultrasonic thickness testing and radiant zone pyrometry inspection of Crude Distillation Unit Furnace F-101, radiant tube skin temperatures and wall thinning rates were observed breaching safe operating limits.

# 2. Verified Inspection Findings

| Parameter / Instrument | Measured Value | Safe Operating Limit | Compliance Status |
| --- | --- | --- | --- |
| Thermocouple TT-104 (Skin Temp) | 620 °C | 610 °C Max | BREACH (>10 °C Over Limit) |
| Ultrasonic Wall Thickness | 4.55 mm (0.45 mm/yr thinning) | 5.00 mm Min | WARNING |
| Burner Firing Rate | 104% MCR | 100% MCR | EXCEEDED |
| Radiant Zone B Flame Impingement | Localized Hotspot Detected | No Impingement | DEFECT |

# 3. Standard Operating Procedure (SOP) Compliance Verdict

MANDATORY CLAUSE 4.1.2 TRIGGERED:
SOP-MRPL-FURNACE-01 dictates that radiant tube skin temperatures exceeding 610°C mandate an immediate firing rate de-rating to ≤85% MCR and execution of an emergency decoking turnaround within 7 calendar days.

# 4. Recommended Authority Action

1. Approve immediate throughput de-rating of CDU-1 from 104% to 80% MCR.

2. Schedule emergency on-line spalling / decoking turnaround for Furnace F-101.

# 5. Approval Authority Sign-offs

| Initiated By: ___________________ Senior Operations Engineer (CDU-1) | Reviewed By: ___________________ Chief General Manager (Technical Services) | Approved By: ___________________ Executive Director (Refinery Operations) |
| --- | --- | --- |